| طرح نگهداشت و افزایش تولید 27 مخزن |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| W.P.S & P.Q.R نگهداشت و افزایش تولید میدان نفتی بینک |  |  |  |  |  |  |  |
| V00 | Mar. 2024 | IFA | AAC | M.FAKHARIAN | S.FRAMARZPOUR |  |
| Rev. | Date | Purpose of Issue/Status | Prepared by: | Checked by: | Approved by: | CLIENT Approval |
| Status: | IFA: Issued For Approval IFI: Issued For Information AFC: Approved For Construction |  |  |  |  |  |

REVISION RECORD SHEET

| PAGE | V00 | V01 | V02 | V03 | V04 |  | PAGE | V00 | V01 | V02 | V03 | V04 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | X |  |  |  |  |  | 66 |  |  |  |  |  |
| 2 | X |  |  |  |  |  | 67 |  |  |  |  |  |
| 3 | X |  |  |  |  |  | 68 |  |  |  |  |  |
| 4 | X |  |  |  |  |  | 69 |  |  |  |  |  |
| 5 | X |  |  |  |  |  | 70 |  |  |  |  |  |
| 6 | X |  |  |  |  |  | 71 |  |  |  |  |  |
| 7 | X |  |  |  |  |  | 72 |  |  |  |  |  |
| 8 | X |  |  |  |  |  | 73 |  |  |  |  |  |
| 9 | X |  |  |  |  |  | 74 |  |  |  |  |  |
| 10 | X |  |  |  |  |  | 75 |  |  |  |  |  |
| 11 | X |  |  |  |  |  | 76 |  |  |  |  |  |
| 12 | X |  |  |  |  |  | 77 |  |  |  |  |  |
| 13 | X |  |  |  |  |  | 78 |  |  |  |  |  |
| 14 |  |  |  |  |  |  | 79 |  |  |  |  |  |
| 15 |  |  |  |  |  |  | 80 |  |  |  |  |  |
| 16 |  |  |  |  |  |  | 81 |  |  |  |  |  |
| 17 |  |  |  |  |  |  | 82 |  |  |  |  |  |
| 18 |  |  |  |  |  |  | 83 |  |  |  |  |  |
| 19 |  |  |  |  |  |  | 84 |  |  |  |  |  |
| 20 |  |  |  |  |  |  | 85 |  |  |  |  |  |
| 21 |  |  |  |  |  |  | 86 |  |  |  |  |  |
| 22 |  |  |  |  |  |  | 87 |  |  |  |  |  |
| 23 |  |  |  |  |  |  | 88 |  |  |  |  |  |
| 24 |  |  |  |  |  |  | 89 |  |  |  |  |  |
| 25 |  |  |  |  |  |  | 90 |  |  |  |  |  |
| 26 |  |  |  |  |  |  | 91 |  |  |  |  |  |
| 27 |  |  |  |  |  |  | 92 |  |  |  |  |  |
| 28 |  |  |  |  |  |  | 93 |  |  |  |  |  |
| 29 |  |  |  |  |  |  | 94 |  |  |  |  |  |
| 30 |  |  |  |  |  |  | 95 |  |  |  |  |  |
| 31 |  |  |  |  |  |  | 96 |  |  |  |  |  |
| 32 |  |  |  |  |  |  | 97 |  |  |  |  |  |
| 33 |  |  |  |  |  |  | 98 |  |  |  |  |  |
| 34 |  |  |  |  |  |  | 99 |  |  |  |  |  |
| 35 |  |  |  |  |  |  | 100 |  |  |  |  |  |
| 36 |  |  |  |  |  |  | 101 |  |  |  |  |  |
| 37 |  |  |  |  |  |  | 102 |  |  |  |  |  |
| 38 |  |  |  |  |  |  | 103 |  |  |  |  |  |
| 39 |  |  |  |  |  |  | 104 |  |  |  |  |  |
| 40 |  |  |  |  |  |  | 105 |  |  |  |  |  |
| 41 |  |  |  |  |  |  | 106 |  |  |  |  |  |
| 42 |  |  |  |  |  |  | 107 |  |  |  |  |  |
| 43 |  |  |  |  |  |  | 108 |  |  |  |  |  |
| 44 |  |  |  |  |  |  | 109 |  |  |  |  |  |
| 45 |  |  |  |  |  |  | 110 |  |  |  |  |  |
| 46 |  |  |  |  |  |  | 111 |  |  |  |  |  |
| 47 |  |  |  |  |  |  | 112 |  |  |  |  |  |
| 48 |  |  |  |  |  |  | 113 |  |  |  |  |  |
| 49 |  |  |  |  |  |  | 114 |  |  |  |  |  |
| 50 |  |  |  |  |  |  | 115 |  |  |  |  |  |
| 51 |  |  |  |  |  |  | 116 |  |  |  |  |  |
| 52 |  |  |  |  |  |  | 117 |  |  |  |  |  |
| 53 |  |  |  |  |  |  | 118 |  |  |  |  |  |
| 54 |  |  |  |  |  |  | 119 |  |  |  |  |  |
| 55 |  |  |  |  |  |  | 120 |  |  |  |  |  |
| 56 |  |  |  |  |  |  | 121 |  |  |  |  |  |
| 57 |  |  |  |  |  |  | 122 |  |  |  |  |  |
| 58 |  |  |  |  |  |  | 123 |  |  |  |  |  |
| 59 |  |  |  |  |  |  | 124 |  |  |  |  |  |
| 60 |  |  |  |  |  |  | 125 |  |  |  |  |  |
| 61 |  |  |  |  |  |  | 126 |  |  |  |  |  |
| 62 |  |  |  |  |  |  | 127 |  |  |  |  |  |
| 63 |  |  |  |  |  |  | 128 |  |  |  |  |  |
| 64 |  |  |  |  |  |  | 129 |  |  |  |  |  |
| 65 |  |  |  |  |  |  | 130 |  |  |  |  |  |

CONTENTS

| 1.0 | INTRODUCTION | 4 |
| --- | --- | --- |
| 2.0 | WPS& PQR | 5 |

- INTRODUCTION

Binak oilfield in Bushehr province is a part of the southern oilfields of Iran, is located 20 km northwest of Genaveh city.

With the aim of increasing production of oil from Binak oilfield, an EPC/EPD Project has been defined by NIOC/NISOC and awarded to Petro Iran Development Company (PEDCO). Also PEDCO (as General Contractor) has assigned the EPC-packages of the Project to "Hirgan Energy - Design and Inspection" JV.

GENERAL DEFINITION

The following terms shall be used in this document.

| CLIENT: | National Iranian South Oilfields Company (NISOC) |
| --- | --- |
| PROJECT: | Binak Oilfield Development – Manufacturing (w/Engineering & Material Supply) of Air Coolers |
| EPD/EPC CONTRACTOR (GC): | Petro Iran Development Company (PEDCO) |
| OWNER: | OWNER is collectively refer to National Iranian South Oil Company (NISOC) and Petro Iran Development Company (PEDCO) |
| EPC CONTRACTOR: | Joint Venture of : Hirgan Energy – Design & Inspection(D&I) Companies |
| VENDOR: | Aban Air Cooler (AAC) |
| EXECUTOR: | Executor is the party which carries out all or part of construction and/or commissioning for the project. |
| THIRD PARTY INSPECTOR (TPI): | Third Party Inspector |
| SHALL: | Is used where a provision is mandatory. |
| SHOULD: | Is used where a provision is advisory only. |
| WILL: | Is normally used in connection with the action by CLIENT rather than by an EPC/EPD CONTRACTOR, supplier or VENDOR. |
| MAY: | Is used where a provision is completely discretionary. |

- wps&pqr

| # CONTENT | # Page NO. |
| --- | --- |
| # WPS NO.: |  |
| # WPS-17208-01 | # 6 |
| # WPS-17208-02 | # 8 |
| # WPS-17208-03 | # 10 |
| # WPS-17208-04 | # 12 |
| # PQR NO.: |  |
| # PQR-31-03-022-27077 | # 14 |
| # PQR-37-00-04-1inch - Manual | # 22 |

# WPS-17208-01:

| WPS No.: WPS-17208-01 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Supporting PQR No.: PQR-31-03-02/2-27077 Welding Process: SAW Type: Automatic (SAW) |  |  |  | Code/Specification: ASME Sec. IX, Last edition |  |
| Joints (QW-402) |  |  |  |  |  |
| Joint Design: See the Sketch Tube /Plug Sheet to Top/Bottom Plate Backing: Yes ■ (SAW) No □ Backing Metal (Type): Weld Metal for top& bottom plate tube sheet Ceramic for partition plate Type of Joint: Groove, Fillet Other: Note: This is a schematic joint design. Beveling and Edge preparation shall be performed in accordance with related detail DWG's. |  |  |  |  |  |
| Base Metals (QW-403) |  |  |  |  |  |
| P No.: 8 Gr. No.: 1 To P No.: 8 Gr. No.: 1 Specification Type and Grade: SA-240 TP316L to SA-240 TP316L. |  |  | Qualified Base Metal Range: Groove: 5-200 mm Fillet: All Maximum Pass Thickness ≤ 1/2 in. (13 mm): Yes■ No□ Pipe Diameter Range: NA Groove: Fillet: Other: |  |  |
| Filler Metals (QW-404) |  |  |  |  |  |
|  | Backing Pass (SAW) |  |  |  | Filling Pass (SAW) |
| Specification No. of electrode or filler | SFA 5.9 |  |  |  | SFA 5.9 |
| AWS No. (Class) | ER 316L |  |  |  | ER 316L |
| F. No. | 6 |  |  |  | 6 |
| A. No. | 8 |  |  |  | 8 |
| Size of Filler Metal | Ø=3.2 |  |  |  | Ø=3.2 |
| Qualified Weld Metal Thickness Range: Groove Fillet | Up to 200 mm All |  |  |  | Up to 200 mm All |
| Flux | OP71 Cr |  |  |  | OP71 Cr |
| Brand/Trade Name | AMA |  |  |  | AMA |
| Consumable Insert | AMA 30-53 |  |  |  | AMA 30-53 |
| Other | - |  |  |  | - |
| Note: - Drying Condition: for flux OP71 Cr 2 hours at 300-350 °C - The maximum width of weave shall not exceed two times of the electrode size |  |  |  |  |  |

| WPS No.: WPS-17208-01 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Position (QW-405) |  |  |  |  |  |  |  |  | Post-weld Heat Treatment (QW-407) |  |  |  |  |  |  |  |  |
| Position of Groove: 1G Welding Progression: Up □ Down □ Position of Fillet: 2F |  |  |  |  |  |  |  |  | Heating (°C/hr), max; Cooling (°C/hr), max; Time (min); Temperature (°C). -; -; -; -. |
| Pre-heat (QW-406) |  |  |  |  |  |  |  |  |  | Gas (QW-408) |  |  |  |  |  |  |  |
| Pre-heat Temperature: Ambient Maximum Inter Pass Temperature: 175 °C Preheat Maintenance: - |  |  |  |  |  |  |  |  |  | Type |  | mixture |  |  | Flow rate |  |  |
|  |  |  |  |  |  |  |  |  |  | - |  | - |  |  | - |  |  |
| Electrical Characteristic (QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Current: AC □ DC ■ Amperage Range: Refer to below table (Amperage and Voltage range should be based on electrode size, position and thickness and etc.) |  |  |  |  |  |  |  | Polarity: RP Tungsten Electrode Size and Type: NA Mode of Metal Transfer and GMAW: NA Electrode Wire Feed Speed Range: NA |  |  |  |  |  |  |  |  |  |
| Technique |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| String or Weave Bead: Orifice of Gas Cup Size: Initial and Inter Pass Cleaning: Method of Back Gouging: Oscillation: Contact Tube Work Distance: Multiple or Single Pass: Multiple or Single Electrode: Travel Speed (Range): Peening |  |  |  |  |  |  |  |  |  | String NA Brushing ■ Grinding ■ Other □ Machining NA 30 mm Multiple Single See below Not permitted |  |  |  |  |  |  |  |
|  | Weld Layers | Process |  | Filler Metal |  |  | Current |  |  | Voltage |  |  |  | Travel Speed Range (cm/min) |  | Heat Input (kJ/cm) | Others |
|  |  |  |  | Class |  | Dia. (mm) | Polarity |  | Amp. |  |  |  |  |  |  |  |  |
| Weld Metal backing | 1 (Back) | SAW |  | ER 316L |  | 3.2 | DCRP |  | 300-500 | 22-28 |  |  |  | 20-40 |  | 9.9-33.6 |  |
|  | 2-n | SAW |  | ER 316L |  | 3.2 | DCRP |  | 300-500 | 22-28 |  |  |  | 20-40 |  | 9.9-33.6 |  |
| Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Weld Metal backing | Step |  | Description |  | Weld type |  | Cleaning |  |  |  | NDT |  | Position |  |  |  |  |
|  | 1 |  | Back Weld |  | Fillet |  | Brushing before welding |  |  |  | - |  | 2F |  |  |  |  |
|  | 2 |  | Machining |  | - |  | - |  |  |  | - |  | - |  |  |  |  |
|  | 3 |  | NDT |  | - |  | - |  |  |  | PT |  | - |  |  |  |  |
|  | 4 |  | Root and Filling pass |  | Groove |  | Brushing between welding passes |  |  |  | - |  | 1G |  |  |  |  |
|  | 5 |  | NDT |  | - |  | - |  |  |  | NDT map |  | - |  |  |  |  |

WPS-17208-02:

| WPS No.: WPS-17208-02 |  |  |  |  |
| --- | --- | --- | --- | --- |
| Supporting PQR No.: PQR-31-03-02/2-27077 Welding Process: GTAW+SAW Type: Automatic (SAW), Manual (GTAW) |  |  |  | Code/Specification: ASME Sec. IX, Last edition |
| Joints (QW-402) |  |  |  |  |
| Joint Design: See the Sketch End Plate to Tube/Plug Sheet End Plate to top and bottom plate Backing: Yes ■ No □ Backing Type: No (GTAW), Weld metal for (SAW) Type of Joint: Groove, fillet Other: Note: This is a schematic joint design. Beveling and Edge preparation shall be performed in accordance with related detail DWG's. |  |  |  |  |
| Base Metals (QW-403) |  |  |  |  |
| P No.: 8 Gr. No.: 1 To P No.: 8 Gr. No.: 1 Specification Type and Grade: SA-240 TP316L to SA-240 TP316L. |  |  | Qualified 01 01 Base Metal Range: Groove: 5-200 mm Fillet: All Maximum Pass Thickness ≤ 1/2 in. (13 mm): 01 01 01 01 Yes ■ No □ Pipe Diameter Range: NA Groove: Fillet: Other: |  |
| Filler Metals (QW-404) |  |  |  |  |
|  | Root Pass (GTAW) |  |  | Filling Pass (SAW) |
| Specification No. of electrode or filler | SFA 5.9 |  |  | SFA 5.9 |
| AWS No. (Class) | ER 316L |  |  | ER 316L |
| F. No. | 6 |  |  | 6 |
| A. No. | 8 |  |  | 8 |
| Size of Filler Metal | Ø=2.4 |  |  | Ø=3.2 |
| Qualified Weld Metal Thickness Range: Groove Fillet | Up to 6 mm All |  |  | Up to 200 mm All |
| Flux | - |  |  | OP71 Cr |
| Brand/Trade Name | AMA |  |  | AMA |
| Consumable Insert | AMA 30-13T |  |  | AMA 30-53 |
| Other | - |  |  | - |
| Note: - Drying Condition: for flux OP71 Cr 2 hours at 300-350 °C - The maximum width of weave shall not exceed two times of the electrode size. |  |  |  |  |

| WPS No.: WPS-17208-02 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Position (QW-405) |  |  |  |  |  |  |  | Post-weld Heat Treatment (QW-407) |  |  |  |  |  |  |  |  |
| Position of Groove: 1G Welding Progression: Up □ Down □ Position of Fillet: -- |  |  |  |  |  |  |  | Heating (°C/hr), max; Cooling (°C/hr), max; Time (min); Temperature (°C). -; -; -; -. |
| Pre-heat (QW-406) |  |  |  |  |  |  |  | Gas (QW-408) |  |  |  |  |  |  |  |  |
| Pre-heat Temperature: 10 °C Maximum Inter Pass Temperature: 175 °C Preheat Maintenance: - |  |  |  |  |  |  |  | Type |  |  |  | Mixture ASME/AWS SFA/A5.32/5.32M |  |  | Flow rate(L/min) |  |
|  |  |  |  |  |  |  |  | Shielding |  |  |  | 99.99% |  |  | 4-8 |  |
|  |  |  |  |  |  |  |  | Tracing |  |  |  | - |  |  | - |  |
|  |  |  |  |  |  |  |  | Backing |  |  |  | 99.99% |  |  | 8-10 |  |
| Electrical Characteristic (QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Current: AC □ DC ■ Amperage Range: Refer to below table (Amperage and Voltage range should be based on electrode size, position and thickness and etc.) |  |  |  |  |  |  | Polarity: SP(GTAW) & RP(SAW) Tungsten Electrode Size and Type: 2.4 mm – EWTH-2 Mode of Metal Transfer and GMAW: NA Electrode Wire Feed Speed Range: NA |  |  |  |  |  |  |  |  |  |
| Technique |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| String or Weave Bead: Orifice of Gas Cup Size: Initial and Inter Pass Cleaning: Method of Back Gouging: Oscillation: Contact Tube Work Distance: Multiple or Single Pass: Multiple or Single Electrode: Travel Speed (Range): Peening Other: |  |  |  |  |  |  |  | Both (GTAW), String (SAW) 8-10 mm Brushing ■ Grinding ■ Other □ NA NA 30 mm (SAW) Multiple Single See below Not permitted - |  |  |  |  |  |  |  |  |
| Weld Layers |  | Process | Filler Metal |  | Current |  |  | Voltage |  | Travel Speed Range (cm/min) |  |  |  | Heat Input (kJ/cm) |  | Others |
|  |  |  | Class | Dia. (mm) | Polarity | Amp. |  |  |  |  |  |  |  |  |  |  |
| 1-2 |  | GTAW | ER 316L | 2.4 | DCSP | 70-130 |  | 7-13 |  | 5-10 |  |  |  | 4.2-20.1 |  |  |
| 3-n |  | SAW | ER 316L | 3.2 | DCRP | 300-500 |  | 22-28 |  | 20-40 |  |  |  | 9.9-33.6 |  |  |
| Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Step | Description |  | Weld type | Cleaning |  |  |  |  | NDT |  | Position |  |  |  |  |  |
| 1 | Root pass |  | Groove | Brushing before welding |  |  |  |  | - |  | 1G |  |  |  |  |  |
| 2 | NDT |  | - | Brushing after grinding |  |  |  |  | PT |  | - |  |  |  |  |  |
| 3 | Filling pass |  | Groove | Brushing between welding passes |  |  |  |  | - |  | 1G |  |  |  |  |  |
| 4 | NDT |  | - | - |  |  |  |  | NDT map |  | - |  |  |  |  |  |

| WPS-17208-03: |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| WPS No.: WPS-17208-03 |  |  |  |  |  |
| Supporting PQR No.: PQR-31-03-02/2-27077 Welding Process: GTAW+SMAW Type: Manual |  |  |  | Code/Specification: ASME Sec. IX, Last edition |  |
| Joints (QW-402) |  |  |  |  |  |
| Joint Design: See the Sketch Pipe Nozzle to Top/Bottom Plate, Flange to Transition Nozzle, Partition Plate to Tube/Plug Sheet. Backing: Yes ■ (Groove: Yes Fillet : Yes) No □ Backing Type: No (GTAW) Yes (SMAW) Type of Joint: Groove & Fillet Other: Note: This is a schematic joint design. Beveling and Edge preparation shall be performed in accordance with related detail DWG's. |  |  |  |  |  |
| Base Metals (QW-403) |  |  |  |  |  |
| P No.: 8 Gr. No.: 1 To P No.: 8 Gr. No.: 1 Specification Type and Grade: SA-240 TP316L to SA-240 TP316L, SA-312 TP316L to SA-182 F316L, SA-240 TP316L to SA-312 TP316L |  |  | Qualified Base Metal Range: Groove: 5-22 mm Fillet: All Maximum Pass Thickness ≤ 1/2 in. (13 mm): Yes ■ No □ Pipe Diameter Range: NA Groove: Fillet: Other: |  |  |
| Filler Metals (QW-404) |  |  |  |  |  |
|  | Root Pass (GTAW) |  |  |  | Filling Pass (SMAW) |
| Specification No. of electrode or filler | SFA 5.9 |  |  |  | SFA 5.4 |
| AWS No. (Class) | ER 316L |  |  |  | E 316L-16 |
| F. No. | 6 |  |  |  | 5 |
| A. No. | 8 |  |  |  | 8 |
| Size of Filler Metal | Ø=3.2 |  |  |  | Ø=3.2 & 4 |
| Qualified Weld Metal Thickness Range: Groove Fillet | Up to 6 mm All |  |  |  | Up to 16 mm all |
| Flux | - |  |  |  | - |
| Brand/Trade Name | AMA |  |  |  | AMA |
| Consumable Insert | AMA 30-13T |  |  |  | AMA 1460JB |
| Other | - |  |  |  | - |
| Note: 1) Drying Condition: for electrode E 316L-16 2 hours at 350-400 °C 2) The maximum width of weave shall not exceed two times of the electrode size. |  |  |  |  |  |

| WPS No.: WPS-17208-03 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Position (QW-405) |  |  |  |  |  |  |  |  | Post-weld Heat Treatment (QW-407) |  |  |  |  |  |  |  |  |  |
| Position of Groove: 1G Welding Progression: Up □ Down □ Position of Fillet: 2F |  |  |  |  |  |  |  |  | Heating (°C/hr), max; Cooling (°C/hr), max; Time (min); Temperature (°C). -; -; -; -. |
| Pre-heat (QW-406) |  |  |  |  |  |  |  |  | Gas (QW-408) |  |  |  |  |  |  |  |  |  |
| Pre-heat Temperature: Ambient Maximum Inter Pass Temperature: 150 °C |  |  |  |  |  |  |  |  | Type |  |  |  | Mixture ASME/AWS SFA/A5.32/5.32M |  |  |  | Flow rate (l/min) |  |
|  |  |  |  |  |  |  |  |  | Shielding |  |  |  | 99.99% |  |  |  | 10-12 |  |
|  |  |  |  |  |  |  |  |  | Tracing |  |  |  | - |  |  |  | - |  |
|  |  |  |  |  |  |  |  |  | Backing |  |  |  | 99.99% |  |  |  | 4-5 |  |
| Electrical Characteristic (QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Current: AC □ DC ■ Amperage Range: Refer to below table (Amperage and Voltage range should be based on electrode size, position and thickness and etc.) |  |  |  |  |  |  |  |  | Polarity: SP(GTAW) & RP(SMAW) Tungsten Electrode Size and Type: 2.4 mm – EWTH-2 Mode of Metal Transfer and GMAW: NA Electrode Wire Feed Speed Range: NA |  |  |  |  |  |  |  |  |  |
| Technique |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| String or Weave Bead: Orifice of Gas Cup Size: Initial and Inter Pass Cleaning: Method of Back Gouging: Oscillation: Contact Tube Work Distance: Multiple or Single Pass: Multiple or Single Electrode: Travel Speed (Range): Peening: Other: |  |  |  |  |  |  |  |  |  | Both 8-10 mm Brushing ■ Grinding ■ Other □ NA NA NA Multiple Single See below Not permitted - |  |  |  |  |  |  |  |  |
| Weld Layers | Process |  | Filler Metal |  |  |  | Current |  |  | Voltage |  | Travel Speed Range (cm/min) |  |  |  | Heat Input (kJ/cm) |  | Others |
|  |  |  | Class |  | Dia. (mm) |  | Polarity | Amp. |  |  |  |  |  |  |  |  |  |  |
| 1-2 | GTAW |  | ER 316L |  | 2.4 |  | DCSP | 70-140 |  | 10-12 |  | 5-10 |  |  |  | 4.2-20.16 |  |  |
| 3 | SMAW |  | E 316L-16 |  | 3.2 |  | DCRP | 70-120 |  | 20-25 |  | 10-20 |  |  |  | 4.2-18 |  |  |
| 4-n | SMAW |  | E 316L-16 |  | 4 |  | DCRP | 100-150 |  | 20-25 |  | 10-20 |  |  |  | 12-22.5 |  |  |
| Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Step |  | Description |  | Weld type |  | Cleaning |  |  |  |  | NDT |  |  | Position |  |  |  |  |
| 1 |  | Root pass |  | Groove, Groove & Fillet |  | Brushing before welding |  |  |  |  | - |  |  | 1G, 2F |  |  |  |  |
| 2 |  | NDT |  | - |  | Brushing after grinding |  |  |  |  | PT |  |  | - |  |  |  |  |
| 3 |  | Filling passes |  | Groove, Groove & Fillet |  | Brushing between welding passes |  |  |  |  | - |  |  | 1G, 2F |  |  |  |  |
| 4 |  | NDT |  | - |  | - |  |  |  |  | NDT map |  |  | - |  |  |  |  |

# WPS-17208-04:

| WPS No.: WPS-17208-04 |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| Supporting PQR No.: PQR-(Orbital)-G1.G2-NHT Welding Process: GTAW Type: Manual |  |  | Code/Specification: ASME Sec. IX, edition 2013 |  |  |
| Joints (QW-402) |  |  |  |  |  |
| Joint Design: See the Sketch Tube to tube sheet Backing: Yes ■ No □ Backing Type: Base metal Type of Joint: Fillet and Groove Other: Depth of Groove: As per related DWGs. |  |  |  |  |  |
| Base Metals (QW-403) |  |  |  |  |  |
| P No.: 8 Gr. No.: 1 To P No.: 8 Gr. No.: 1 Specification Type and Grade: SA-213 TP316L to SA-240 TP316L Tube sheet thickness: 20 mm Tube diameter/thickness: 25.4 mm /1.651 mm |  |  |  | Base Metal Range: Groove: 0.825-3.3 (For Tubes) Fillet: All (For Tubes) Pipe Diameter Range: NA Groove: Fillet: Other: |  |
| Filler Metals (QW-404) |  |  |  |  |  |
|  | All Passes (GTAW) |  |  |  |  |
| Specification No. of electrode or filler | SFA 5.9 |  |  |  |  |
| AWS No. (Class) | ER 316L |  |  |  |  |
| F. No. | 6 |  |  |  |  |
| A. No. | 8 |  |  |  |  |
| Size of Filler Metal | Ø= 1.6 |  |  |  |  |
| Weld Metal Thickness Range: Groove Fillet |  |  |  |  |  |
|  | 0.825-3.3 |  |  |  |  |
|  | All |  |  |  |  |
| Flux | - |  |  |  |  |
| Brand/Trade Name | AMA |  |  |  |  |
| Consumable Insert | AMA 30-13T |  |  |  |  |
| Other (product form) | Rod |  |  |  |  |
| Note: - PT must be done after root pass welding - The maximum width of weave shall not exceed two times of the electrode size. |  |  |  |  |  |

| WPS No.: WPS-17208-04 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Position (QW-405) |  |  |  |  |  |  |  |  |  | Post-weld Heat Treatment (QW-407) |  |  |  |  |  |  |  |  |  |  |
| Position of Groove: - Welding Progression: Up □ Down □ Orbital ■ Position of Fillet: 5F |  |  |  |  |  |  |  |  |  | Temperature Range: NA Heating/Cooling Rate: NA Soaking Time: NA |  |  |  |  |  |  |  |  |  |  |
| Pre-heat (QW-406) |  |  |  |  |  |  |  |  |  | Gas (QW-408) |  |  |  |  |  |  |  |  |  |  |
| Pre-heat Temperature: Ambient Maximum Inter Pass Temperature: 150 °C Preheat Maintenance: - (Continuous or Special heating where applicable should be recorded) |  |  |  |  |  |  |  |  |  | Type |  |  | Gas |  | Mixture ASME/AWS SFA/A5.32/5.32M |  |  | Flow rate (l/min) |  |  |
|  |  |  |  |  |  |  |  |  |  | Shielding |  |  | Argon |  | 99.99% |  |  | 10-12 |  |  |
|  |  |  |  |  |  |  |  |  |  | Tracing |  |  | - |  | - |  |  | - |  |  |
|  |  |  |  |  |  |  |  |  |  | Backing |  |  | - |  | - |  |  | - |  |  |
| Electrical Characteristic (QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Current: AC □ DC ■ Amperage Range: Refer to below table (Amperage and Voltage range should be based on electrode size, position and thickness and etc.) |  |  |  |  |  |  |  |  | Polarity: SP Tungsten Electrode Size and Type: 1.6 mm – EWTH-2 Mode of Metal Transfer and GMAW: NA Electrode Wire Feed Speed Range: NA |  |  |  |  |  |  |  |  |  |  |  |
| Technique |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| String or Weave Bead: Orifice of Gas Cup Size: Initial and Inter Pass Cleaning: Method of Back Gouging: Oscillation: Contact Tube Work Distance: Multiple or Single Pass: Multiple or Single Electrode: Travel Speed (Range): |  |  |  |  |  |  |  | String - Brushing □ Grinding □ Other ■:(Suitable solvent cleaning) NA NA NA Multiple Single See below |  |  |  |  |  |  |  |  |  |  |  |  |
| Weld Layers |  | Process | Filler Metal |  |  |  | Current |  |  |  |  |  |  | Voltage |  |  | Travel Speed Range (cm/min) |  | Heat Input (KJ/cm) | Others |
|  |  |  | Class |  | Dia. (mm) |  | Polarity |  |  |  | Amp. |  |  |  |  |  |  |  |  |  |
| 1 |  | GTAW | ER 316L |  | 1.6 |  | DCSP |  |  |  | 70-120 |  |  | 10-12 |  |  | 5-10 |  | 8.4-17.3 |  |
| Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Step | Description |  |  | Weld type |  | Cleaning |  |  |  |  |  | NDT |  | Position |  |  |  |  |  |  |
| 1 | Root pass |  |  | Groove |  | Brushing before welding |  |  |  |  |  | - |  | 5F |  |  |  |  |  |  |
| 3 | NDT |  |  | - |  | - |  |  |  |  |  | NDT map |  | - |  |  |  |  |  |  |