| طرح نگهداشت و افزایش تولید 27 مخزن |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| WPS & PQR نگهداشت و افزایش تولید میدان نفتی بینک |  |  |  |  |  |  |
| V02 | Mar.2025 | IFR | Beh Koosh Vista | M.Fakharian | S. Faramaz Pour |  |
| V01 | Oct.2023 | IFR | Beh Koosh Vista | M.Fakharian | S. Faramaz Pour |  |
| V00 | Aug.2023 | IFR | Beh Koosh Vista | M.Fakharian | A.M.Mohseni | CO |
| Rev. | Date | Purpose of Issue/Status | Prepared by: | Checked by: | Approved by: | CLIENT Approval |
| Class: 2 |  |  |  |  |  |  |
| Status: | IFA: Issued for Approval IFR: Issued for Review IFI: Issued for Information AFC: Approved for Construction. |

# Revision Record Sheet

| SHEET | V00 | V01 | V02 | V03 | V04 | V05 | V06 | V07 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 1 | X |  |  |  |  |  |  |  |
| 2 | X |  |  |  |  |  |  |  |
| 3 | X | X |  |  |  |  |  |  |
| 4 | X | X | X |  |  |  |  |  |
| 5 | X | X | X |  |  |  |  |  |
| 6 | X | X | X |  |  |  |  |  |
| 7 | X |  |  |  |  |  |  |  |
| 8 | X |  |  |  |  |  |  |  |
| 9 | X |  |  |  |  |  |  |  |
| 10 | X |  | X |  |  |  |  |  |
| 11 | X |  |  |  |  |  |  |  |
| 12 | X |  |  |  |  |  |  |  |
| 13 | X |  |  |  |  |  |  |  |
| 14 | X |  |  |  |  |  |  |  |
| 15 | X |  |  |  |  |  |  |  |
| 16 | X |  |  |  |  |  |  |  |
| 17 | X |  |  |  |  |  |  |  |
| 18 |  |  |  |  |  |  |  |  |
| 19 |  |  |  |  |  |  |  |  |
| 20 |  |  |  |  |  |  |  |  |
| 21 |  |  |  |  |  |  |  |  |
| 22 |  |  |  |  |  |  |  |  |
| 23 |  |  |  |  |  |  |  |  |
| 24 |  |  |  |  |  |  |  |  |
| 25 |  |  |  |  |  |  |  |  |
| 26 |  |  |  |  |  |  |  |  |
| 27 |  |  |  |  |  |  |  |  |
| 28 |  |  |  |  |  |  |  |  |
| 29 |  |  |  |  |  |  |  |  |
| 30 |  |  |  |  |  |  |  |  |
| 31 |  |  |  |  |  |  |  |  |
| 32 |  |  |  |  |  |  |  |  |
| 33 |  |  |  |  |  |  |  |  |
| 34 |  |  |  |  |  |  |  |  |
| 35 |  |  |  |  |  |  |  |  |
| 36 |  |  |  |  |  |  |  |  |
| 37 |  |  |  |  |  |  |  |  |
| 38 |  |  |  |  |  |  |  |  |
| 39 |  |  |  |  |  |  |  |  |
| 40 |  |  |  |  |  |  |  |  |
| 41 |  |  |  |  |  |  |  |  |
| 42 |  |  |  |  |  |  |  |  |
| 43 |  |  |  |  |  |  |  |  |
| 44 |  |  |  |  |  |  |  |  |
| 45 |  |  |  |  |  |  |  |  |
| 46 |  |  |  |  |  |  |  |  |
| 47 |  |  |  |  |  |  |  |  |
| 48 |  |  |  |  |  |  |  |  |
| 49 |  |  |  |  |  |  |  |  |
| 50 |  |  |  |  |  |  |  |  |

| SHEET | V00 | V01 | V02 | V03 | V04 | V05 | V06 | V07 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 51 |  |  |  |  |  |  |  |  |
| 52 |  |  |  |  |  |  |  |  |
| 53 |  |  |  |  |  |  |  |  |
| 54 |  |  |  |  |  |  |  |  |
| 55 |  |  |  |  |  |  |  |  |
| 56 |  |  |  |  |  |  |  |  |
| 57 |  |  |  |  |  |  |  |  |
| 58 |  |  |  |  |  |  |  |  |
| 59 |  |  |  |  |  |  |  |  |
| 60 |  |  |  |  |  |  |  |  |
| 61 |  |  |  |  |  |  |  |  |
| 62 |  |  |  |  |  |  |  |  |
| 63 |  |  |  |  |  |  |  |  |
| 64 |  |  |  |  |  |  |  |  |
| 65 |  |  |  |  |  |  |  |  |
| 66 |  |  |  |  |  |  |  |  |
| 67 |  |  |  |  |  |  |  |  |
| 68 |  |  |  |  |  |  |  |  |
| 69 |  |  |  |  |  |  |  |  |
| 70 |  |  |  |  |  |  |  |  |
| 71 |  |  |  |  |  |  |  |  |
| 72 |  |  |  |  |  |  |  |  |
| 73 |  |  |  |  |  |  |  |  |
| 74 |  |  |  |  |  |  |  |  |
| 75 |  |  |  |  |  |  |  |  |
| 76 |  |  |  |  |  |  |  |  |
| 77 |  |  |  |  |  |  |  |  |
| 78 |  |  |  |  |  |  |  |  |
| 79 |  |  |  |  |  |  |  |  |
| 80 |  |  |  |  |  |  |  |  |
| 81 |  |  |  |  |  |  |  |  |
| 82 |  |  |  |  |  |  |  |  |
| 83 |  |  |  |  |  |  |  |  |
| 84 |  |  |  |  |  |  |  |  |
| 85 |  |  |  |  |  |  |  |  |
| 86 |  |  |  |  |  |  |  |  |
| 87 |  |  |  |  |  |  |  |  |
| 88 |  |  |  |  |  |  |  |  |
| 89 |  |  |  |  |  |  |  |  |
| 90 |  |  |  |  |  |  |  |  |
| 91 |  |  |  |  |  |  |  |  |
| 92 |  |  |  |  |  |  |  |  |
| 93 |  |  |  |  |  |  |  |  |
| 94 |  |  |  |  |  |  |  |  |
| 95 |  |  |  |  |  |  |  |  |
| 96 |  |  |  |  |  |  |  |  |
| 97 |  |  |  |  |  |  |  |  |
| 98 |  |  |  |  |  |  |  |  |
| 99 |  |  |  |  |  |  |  |  |
| 100 |  |  |  |  |  |  |  |  |

Contents

Revision Record Sheet	2

1	Introduction	4

2	Reference Documents	4

3	WPS	5

3.1  WPS NO.:11TA-1………………………………………………………………………………………………………………4

3.2  WPS NO.:11TA-2………………………………………………………………………………………………………………4

3.3  WPS NO.:11A-3………………………………………………………………………………………………………  ………4

4       PQR NO.: PQ-VISTA-102……………………………………………………………………………6

# Introduction

This document describes the welding procedure for all welding attachments of equipment with item No: PL-3201, PR-3201 which are designed and fabricated by Vista Company, following on attached procedure qualification record (PQR).

GENERAL DEFINITION

The following terms shall be used in this document.

| CLIENT: | National Iranian South Oilfields Company (NISOC) |
| --- | --- |
| PROJECT: | Binak Oilfield Development – Manufacturing (w/Engineering & Material Supply) of Pig traps |
| EPD/EPC CONTRACTOR (GC): | Petro Iran Development Company (PEDCO) |
| EPC CONTRACTOR/PURCAHSER: | Joint Venture of: Hirgan Energy – Design & Inspection(D&I) Companies |
| VENDOR: | Nam Avaran Beh Koosh Vista |
| EXECUTOR: | Executor is the party which carries out all or part of construction and/or commissioning for the project. |
| TPI: | Third Party Inspector |

# Reference Documents

Unless stated otherwise all codes and standards referenced in this procedure shall be of the latest issue (including revisions – addenda and supplements) and the following documents shall be referred to along with this procedure.

| ASME Section IX-2019 | -Qualification Standard for Welding, Brazing, and Fusing Procedures; Welders; Brazers; and Welding, Brazing, and Fusing Operators |
| --- | --- |
| ASME B31.8- 2016 | - Gas transmission and distribution piping system |
| ASME Section VIII Div. 1- 2019 | - Boiler & Pressure Vessels code |
| ASME B31.3- 2022 | - Process Piping |
| IPS-M-PI-130 - 2014 | - Material and equipment standard for pig launching and receiving traps |
| NACE MR0175/ISO 15156 | - Petroleum and natural gas industries—Materials for use in H2S-containing environments in oil and gas production |

# WPS

| ### Code & standard: ASME SEC. IX ,ASME SEC. VIII Div.1, ### NACE MR 0175/ISO15156 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Welding Process: GTAW+SMAW |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ### WPS No.: 11TA-1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### PQR No.: PQ-VISTA-102 |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Type : ■ MANUAL □ AUTOMATIC □ SEMI AUTO |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Page : 1 of 3 |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Date : 5.Mar.2025 |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Joint Design Used(QW-402) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Position(QW-405) |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Type of Joint : |  |  | ### Butt Weld (pipe to pipe, closure, flange, reducer) ### ■ Single □ Double Weld |  |  |  |  |  |  |  |  |  |  |  |  | Position Of Groove: |  |  |  |  |  | ALL |  |  |  |  |  |  |
| Backing: |  |  |  |  |  |  |  | □ Yes ■ No |  |  |  |  |  |  |  |  | Weld Progression: |  |  |  | ALL |  |  |  |  |  |  |  |
| Backing Material: |  |  |  |  |  |  |  | --- |  |  |  |  |  |  |  |  | Vertical Progression: |  |  |  | ■Up Down |  |  |  |  |  |  |  |
| Back Chiping: |  |  |  |  |  |  |  | □ Yes ■ No |  |  |  |  |  |  |  |  | ### Postweld Heat Treatment(QW-407) |  |  |  |  |  |  |  |  |  |  |  |
| ### Base Metals(QW-403) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Temperature: 620°C |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (1): |  |  |  | API 5L X52/PSL2 (P No. 1 Gr. No. 1)- NACE MR 0175/ISO 15156 |  |  |  |  |  |  |  |  |  |  |  | Time: 30 min. |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (2): |  |  |  | A-860 WPH 52, A 694 F52 (P No. 1 Gr. No. 1)- NACE MR 0175/ISO 15156 |  |  |  |  |  |  |  |  |  |  |  | ### Preheat(QW-406) |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Thickness: |  |  |  | 9.27 / 8.18 |  |  |  |  |  |  |  |  |  |  |  | Preheat Temp(min): 20°C |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thk. Range: |  |  |  | 5~50.98 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Outside Diameter (Pipe) : 10”, 8 " |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Interpass Temp(max):250°C |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thickness based on thickness of test coupond (T) (QW-451.1) : |  |  |  |  |  |  |  |  |  |  | 5~50 for Base metal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Filler Material(QW-404) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Technique(QW-410) |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Specification/ASME SFA : |  |  |  |  |  |  |  |  | 5.18 |  |  |  | 5.1 |  |  | String Or Weave Bead: String & Weave |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Classification: |  |  |  |  |  |  |  |  | ER70S-6 |  |  |  | E7018 |  |  | Multy Or Single Pass: Multi |  |  |  |  |  |  |  |  |  |  |  |  |
| A. No. : |  |  |  |  |  |  |  |  | 1 |  |  |  | 1 |  |  | Single or Multi Electrodes: Single |  |  |  |  |  |  |  |  |  |  |  |  |
| F. No. : |  |  |  |  |  |  |  |  | 6 |  |  |  | 4 |  |  | Interpass Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |
| Size Of Filler Metal(mm): |  |  |  |  |  |  |  |  | 2.4 |  |  |  | 3.25, 4 |  |  | Initial Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |
| Trade Name: |  |  |  |  |  |  |  |  | 40-16T |  |  |  | 1235F |  |  | Peening:--- |  |  |  |  |  |  |  |  |  |  |  |  |
| Manufacture: |  |  |  |  |  |  |  |  | AMA |  |  |  | AMA |  |  | Oscillation: --- |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thickness range of weld metal: |  |  |  |  |  |  |  |  | Max. 6mm for GTAW |  |  |  | Max. 45mm for SMAW |  |  | Gas |  |  |  | Perecent Composition |  |  |  |  |  |  |  |  |
| Dry Temp. Of Flux: |  |  |  |  |  |  |  |  | --- |  |  |  | --- |  |  |  |  |  |  | Gas(Es) |  |  |  |  |  |  | Gas(Es) | ### Flow |
| Tungsten Electrode |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Shielding Gas(ES) |  |  |  | Ar. 99.99% |  |  |  |  |  |  | Ar. 99.99% | 10-15 Lit/Min |
| Type: |  | ANSI/ASME A5.12-98 |  |  |  |  |  |  |  |  |  |  |  |  |  | Trailing Gas(ES) |  |  |  | ---- |  |  |  |  |  |  | ---- | ---- |
| Size: |  | 2.4 mm *175mm |  |  |  |  |  |  |  |  |  |  |  |  |  | Backing Gas(ES) |  |  |  | ---- |  |  |  |  |  |  | ---- | ---- |
| ### Redry Electrode (Acc. to electrode manufacturer) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Temperature: |  |  |  |  | ### 300-350°C |  |  |  |  |  |  |  |  |  |  | Time: |  |  | 2HR |  |  |  |  |  |  |  |  |  |
| ### Electrical Characteristics(QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| No. | Process |  |  |  |  | Fillter Metal |  |  |  |  |  | Current |  |  |  |  |  |  |  |  |  | Max. each pass thickness (mm) |  |  |  | Travel Speed (Cm/Min) |  | Max. Heat Input (J/mm) |
|  |  |  |  |  |  | Class |  |  |  | Dia.(mm) |  | Type Polar |  |  | Amp.s Range (A) |  |  | Volts Range (V) |  |  |  |  |  |  |  |  |  |  |
| 1 | GTAW |  |  |  |  | ER70S-6 |  |  |  | 2.4 |  | DCEN |  |  | 130 ~ 135 |  |  | 18-20 |  |  |  | 6 |  |  |  | 5-10 |  | 3240 |
| 2 | SMAW |  |  |  |  | E7018 |  |  |  | 3.25 |  | DCEP |  |  | 135 ~ 160 |  |  | 18-20 |  |  |  | 6 |  |  |  | 10-20 |  | 1920 |
| REST | SMAW |  |  |  |  | E7018 |  |  |  | 4 |  | DCEP |  |  | 135 ~ 180 |  |  | 20-23 |  |  |  | 6 |  |  |  | 10-20 |  | 2484 |
| ### Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| - Cleaning & Assembling - Welding of Root Pass - Welding of Filling Pass |  |  |  |  |  |  |  |  |  |  |  |  |  | - Grinding & Brushing - Welding of Filling Pass - Grinding & Brushing |  |  |  |  |  | - Welding of Filling cap - Grinding & Brushing - RT 100% |  |  |  |  |  |  |  |  |

| ### Code & standard: ASME SEC. IX ,ASME SEC. VIII Div.1, ### NACE MR 0175/ISO15156 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Welding Process: GTAW+SMAW |  |  |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ### WPS No.: 11TA-2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### PQR No.: PQ-VISTA-102 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Type : ■ MANUAL □ AUTOMATIC □ SEMI AUTO |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Page : 2 of 3 |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Date : 5.Mar.2025 |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Joint Design Used(QW-402) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Position(QW-405) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Type of Joint : |  |  | ### Butt Weld (Weldolet to Flange, Pipe) ### ■ Single □ Double Weld |  |  |  |  |  |  |  |  |  |  |  |  | Position Of Groove: |  |  |  |  |  |  | ALL |  |  |  |  |  |  |
| Backing: |  |  |  |  |  |  |  | □ Yes ■ No |  |  |  |  |  |  |  |  | Weld Progression: |  |  |  |  | ALL |  |  |  |  |  |  |  |
| Backing Material: |  |  |  |  |  |  |  | --- |  |  |  |  |  |  |  |  | Vertical Progression: |  |  |  |  | ■Up Down |  |  |  |  |  |  |  |
| Back Chiping: |  |  |  |  |  |  |  | □ Yes ■ No |  |  |  |  |  |  |  |  | ### Postweld Heat Treatment(QW-407) |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Base Metals(QW-403) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Temperature: 620°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (1): |  |  | A 105 (P No. 1 Gr. No. 2)- NACE MR 0175/ISO 15156 |  |  |  |  |  |  |  |  |  |  |  |  | Time: 30 min. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (2): |  |  | API 5L X52/PSL2(P No. 1 Gr. No. 1), A 105 (P No. 1 Gr. No. 2)- NACE MR 0175/ISO 15156 |  |  |  |  |  |  |  |  |  |  |  |  | ### Preheat(QW-406) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Thickness: |  |  | 5.54 / 6.35 |  |  |  |  |  |  |  |  |  |  |  |  | Preheat Temp(min): 20°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thk. Range: |  |  |  | 5~50.98 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Outside Diameter (Pipe) : 2”, 1 " |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Interpass Temp(max):250°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thickness based on thickness of test coupond (T) (QW-451.1) : |  |  |  |  |  |  |  |  |  |  | 5~50 for Base metal |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Filler Material(QW-404) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Technique(QW-410) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Specification/ASME SFA : |  |  |  |  |  |  |  |  | 5.18 |  |  | 5.1 |  |  |  | String Or Weave Bead: String & Weave |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Classification: |  |  |  |  |  |  |  |  | ER70S-6 |  |  | E7018 |  |  |  | Multy Or Single Pass: Multi |  |  |  |  |  |  |  |  |  |  |  |  |  |
| A. No. : |  |  |  |  |  |  |  |  | 1 |  |  | 1 |  |  |  | Single or Multi Electrodes: Single |  |  |  |  |  |  |  |  |  |  |  |  |  |
| F. No. : |  |  |  |  |  |  |  |  | 6 |  |  | 4 |  |  |  | Interpass Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size Of Filler Metal(mm): |  |  |  |  |  |  |  |  | 2.4 |  |  | 3.25, 4 |  |  |  | Initial Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Trade Name: |  |  |  |  |  |  |  |  | 40-16T |  |  | 1235F |  |  |  | Peening:--- |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Manufacture: |  |  |  |  |  |  |  |  | AMA |  |  | AMA |  |  |  | Oscillation: --- |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thickness range of weld metal: |  |  |  |  |  |  |  |  | Max. 6mm for GTAW |  |  | Max. 45mm for SMAW |  |  |  | Gas |  |  |  |  | Perecent Composition |  |  |  |  |  |  |  |  |
| Dry Temp. Of Flux: |  |  |  |  |  |  |  |  | --- |  |  | --- |  |  |  |  |  |  |  |  | Gas(Es) |  |  |  |  |  |  | Gas(Es) | ### Flow |
| Tungsten Electrode |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Shielding Gas(ES) |  |  |  |  | Ar. 99.99% |  |  |  |  |  |  | Ar. 99.99% | 10-15 Lit/Min |
| Type: |  | ANSI/ASME A5.12-98 |  |  |  |  |  |  |  |  |  |  |  |  |  | Trailing Gas(ES) |  |  |  |  | ---- |  |  |  |  |  |  | ---- | ---- |
| Size: |  | 2.4 mm *175mm |  |  |  |  |  |  |  |  |  |  |  |  |  | Backing Gas(ES) |  |  |  |  | ---- |  |  |  |  |  |  | ---- | ---- |
| ### Redry Electrode (Acc. to electrode manufacturer) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Temperature: |  |  |  |  | ### 300-350°C |  |  |  |  |  |  |  |  |  |  | Time: |  |  | 2HR |  |  |  |  |  |  |  |  |  |  |
| ### Electrical Characteristics(QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| No. | Process |  |  |  |  | Fillter Metal |  |  |  |  |  |  | Current |  |  |  |  |  |  | Max. each pass thickness (mm) |  |  |  |  |  | Travel Speed (Cm/Min) |  |  | Max. Heat Input (J/mm) |
|  |  |  |  |  |  | Class |  |  |  | Dia.(mm) |  |  | Type Polar |  | Amp.s Range (A) |  |  | Volts Range (V) |  |  |  |  |  |  |  |  |  |  |  |
| 1 | GTAW |  |  |  |  | ER70S-6 |  |  |  | 2.4 |  |  | DCEN |  | 130 ~ 135 |  |  | 18-22 |  | 6 |  |  |  |  |  | 5-10 |  |  | 3240 |
| 2 | SMAW |  |  |  |  | E7018 |  |  |  | 3.25 |  |  | DCEP |  | 135 ~ 160 |  |  | 18-22 |  | 6 |  |  |  |  |  | 10-20 |  |  | 1920 |
| REST | SMAW |  |  |  |  | E7018 |  |  |  | 4 |  |  | DCEP |  | 135 ~ 180 |  |  | 20-24 |  | 6 |  |  |  |  |  | 10-20 |  |  | 2484 |
| ### Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| - Cleaning & Assembling - Welding of Root Pass - Welding of Filling Pass |  |  |  |  |  |  |  |  |  |  |  |  |  | - Grinding & Brushing - Welding of Filling Pass - Grinding & Brushing |  |  |  |  |  |  | - Welding of Filling cap - Grinding & Brushing - RT 100% |  |  |  |  |  |  |  |  |

| ### Code & standard: ASME SEC. IX ,ASME SEC. VIII Div.1, ### NACE MR 0175/ISO15156 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Welding Process: |  |  |  | ### SMAW |  |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| ### WPS No.: 11A-3 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### PQR No.: |  |  |  | ### PQ-VISTA-102 |  |  |  |  |  |  |  |  |  |  |  |
| ### Type : ■ MANUAL □ AUTOMATIC ### □ SEMI AUTO |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Page : |  |  |  | ### 3 of 3 |  |  |  |  |  |  |  |  |  |  |  |
|  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Date : |  |  |  | ### 5.Mar.2025 |  |  |  |  |  |  |  |  |  |  |  |
| ### Joint Design Used(QW-402) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | ### Position(QW-405) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Type of Joint : Fillet Weld ### ■ Single □ Double Weld |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Position Of FILLET: |  |  |  |  |  |  |  | ALL |  |  |  |  |  |
| Backing: |  |  |  |  |  |  |  | ■ Yes □ No |  |  |  |  |  |  |  |  | Weld Progression: |  |  |  |  |  |  |  | UP |  |  |  |  |  |
| Backing Material: |  |  |  |  | BASE METAL |  |  |  |  |  |  |  |  |  |  |  | Vertical Progression: |  |  |  |  |  |  |  | ■Up Down |  |  |  |  |  |
| Back Chiping: |  |  |  |  |  |  |  | □ Yes ■ No |  |  |  |  |  |  |  |  | ### Postweld Heat Treatment(QW-407) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Base Metals(QW-403) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Temperature: 620°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (1): |  |  |  |  |  |  | API 5L X52(P No. 1 Gr. No. 1), /PSL2, A-283 C(P No. 1 Gr. No. 1) |  |  |  |  |  |  |  |  |  | Time: 30 min. |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Spec. (2): |  |  |  |  |  |  | A-283 C(P No. 1 Gr. No. 1) |  |  |  |  |  |  |  |  |  | ### Preheat(QW-406) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Material Thickness: |  |  |  |  |  |  |  |  |  | ALL |  |  |  |  |  |  | Preheat Temp(min): 20°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Qualified Thk. Range: |  |  |  |  |  |  |  |  |  | ALL |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Outside Diameter (Pipe) : -- |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Interpass Temp(max):250°C |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Filler Material(QW-404) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Technique(QW-410) |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Specification/ASME SFA : |  |  |  |  |  |  |  |  |  |  | 5.1 |  |  |  |  |  | String Or Weave Bead: String &Weave |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Aws Classification: |  |  |  |  |  |  |  |  |  |  | E7018 |  |  |  |  |  | Multi Or Single Pass: Multy |  |  |  |  |  |  |  |  |  |  |  |  |  |
| A. No. : |  |  |  |  |  |  |  |  |  |  | 1 |  |  |  |  |  | Single or Multi Electrodes: Single |  |  |  |  |  |  |  |  |  |  |  |  |  |
| F. No. : |  |  |  |  |  |  |  |  |  |  | 4 |  |  |  |  |  | Interpass Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Size Of Filler Metal(mm): |  |  |  |  |  |  |  |  |  |  | 3.25, 4 |  |  |  |  |  | Initial Cleaning: Grinding & Brushing |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Trade Name: |  |  |  |  |  |  |  |  |  |  | 1235F |  |  |  |  |  | Peening:--- |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Manufacture: |  |  |  |  |  |  |  |  |  |  | AMA |  |  |  |  |  | Oscillation: --- |  |  |  |  |  |  |  |  |  |  |  |  |  |
| Flux Trade Name |  |  |  |  |  |  |  |  |  |  | --- |  |  |  |  |  | Gas |  |  |  |  | Perecent Composition |  |  |  |  |  |  |  |  |
| Dry Temp. Of Flux: |  |  |  |  |  |  |  |  |  |  | --- |  |  |  |  |  |  |  |  |  |  | Gas(Es) |  |  |  |  |  | Gas(Es) |  | ### Flow Rate |
| Tungsten Electrode |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Shielding Gas(ES) |  |  |  |  | ---- |  |  |  |  |  | ---- |  | ---- |
| Type: |  | --- |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Trailing Gas(ES) |  |  |  |  | ---- |  |  |  |  |  | ---- |  | ---- |
| Size: |  | --- |  |  |  |  |  |  |  |  |  |  |  |  |  |  | Backing Gas(ES) |  |  |  |  | ---- |  |  |  |  |  | ---- |  | ---- |
| ### Redry Electrode (Acc. to electrode manufacturer) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| ### Temperature: |  |  |  | ### 300-350°C |  |  |  |  |  |  |  |  |  |  |  |  | Time: |  |  | 2HR |  |  |  |  |  |  |  |  |  |  |
| ### Electrical Characteristics(QW-409) |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| No. | Process |  | Fillter Metal |  |  |  |  |  |  |  |  | Current |  |  |  |  |  |  |  |  | Max. each pass thickness (mm) |  |  |  |  | Travel Speed (Cm/Min) |  |  | Max. Heat Input (J/mm) |  |
|  |  |  | Class |  |  |  |  |  | Dia. (mm) |  |  | Type Polar |  |  |  | Amp.s Range (A) |  | Volts Range (V) |  |  |  |  |  |  |  |  |  |  |  |  |
| 1 | SMAW |  | E7018 |  |  |  |  |  | 3.25 |  |  | DCEP |  |  |  | 100-140 |  | 18-22 |  |  | 6 |  |  |  |  | 10-20 |  |  | 1848 |  |
| 2 | SMAW |  | E7018 |  |  |  |  |  | 4 |  |  | DCEP |  |  |  | 120-140 |  | 20-24 |  |  | 6 |  |  |  |  | 10-20 |  |  | 2016 |  |
| ### Welding Sequence |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| - Cleaning & Assembling - Welding of Root Pass - Welding of Filling cap |  |  |  |  |  |  |  |  |  |  |  |  | 4. Grinding & Brushing |  |  |  |  |  |  |  |  |  |  | - MT 100% |  |  |  |  |  |  |